## Slide 1
50 μm
50 μm
50 μm
SEM images of samples reacted at 750°C for (A)5, (B)10, (C)20 and (D)40 minutes, respectively

## Slide 2
Stage 1
Mg2B25
β-B
Mg(g)
Stage 2
Stage 3
Mg2B25
Mg(l)
MgB2
Contact area
∆V=15%
∆V=70%
Mg(l) infiltration
Residual Mg
0< t < 20 min
20 min < t < 1 h
t > 1h
Schematic illustration of microstructure and phase evolution during the IG process

## Slide 3
40 min
2 h
a
b
SEM images of IG processed samples. (A) The sample reacted for 40 minutes shows smaller crack length (shown by arrows). (B) The sample reacted for 2 h shows propagation of cracks and ultimate fracture in Mg2B25 particles (indicated by dotted circles)

## Slide 4
750 ºC
900 ºC
a
b
SEM images of samples reacted for 4 h at (A) 750°C and (B) 900°C. The red arrows indicate the “Diffusion zone”. The purple arrows indicate unreacted Mg and the white arrows indicate the Mg2B25 phase

## Slide 5
Schematic illustration of a progressing Mg2B25 front and the generation of stress

## Slide 6
288K
256K
224K
192K
160K
128K
96K
64K
32K
1.44K
1.28K
1.12K
.96K
.8K
.64K
.48K
.32K
.16K
0 .67 1.34 2.01 2.68 3.35 4.02 4.69 5.36 6.03
0 .67 1.34 2.01 2.68 3.35 4.02 4.69 5.36 6.03
EDS point analysis on spots 1 and 2 (from Figure 1D) showing relative amounts of B and Mg